## Slide 1
SOVEREIGN AIR-GAPPED BRIEFING // CONFIDENTIAL
DECK FOR THIS ANALYSIS.
Executive deliverable compiled for: deck for this analysis.
Date: 01 September 2026 | Sovereign AI Verification Engine

## Slide 2
Executive Overview
Context and Core Objective
• Executive deliverable compiled for: deck for this analysis.
Notes: Speaker Note: Emphasize sovereign on-premises validation.

## Slide 3
Key Findings & Factual Claims
Extracted Evidence
• Findings:
• Line 14-P-102 nominal wall thickness: 12.7 mm
• Operating pressure: 18.5 bar, Operating temperature: 340°C
• Findings:
• Line 14-P-102 nominal wall thickness: 12.7 mm
• Operating pressure: 18.5 bar, Operating temperature: 340°C
Notes: Speaker Note: Walk through each verified claim.

## Slide 4
Critical Statistics & Measurements
Empirical Data Points
• Line 14-P-102 nominal wall thickness: 12.7 mm
• Measured minimum thickness at Elbow EL-04: 6.8 mm due to naphthenic acid corrosion
• Operating pressure: 18.5 bar, Operating temperature: 340°C
• Recommendation: Derate unit operating pressure to 12.0 bar immediately and schedule clamp enclosure installation.
• Line 14-P-102 nominal wall thickness: 12.7 mm
• Measured minimum thickness at Elbow EL-04: 6.8 mm due to naphthenic acid corrosion
Notes: Speaker Note: Focus on quantitative metrics.

## Slide 5
Risk Assessment & Operational Impact
Mitigation Protocols
• [RISK] Measured minimum thickness at Elbow EL-04: 6.8 mm due to naphthenic acid corrosion
• [RISK] High risk of pressure boundary breach under full throughput
• [RISK] Measured minimum thickness at Elbow EL-04: 6.8 mm due to naphthenic acid corrosion
• [RISK] High risk of pressure boundary breach under full throughput
• [RISK] Corrosion rate: 2.8 mm/year
Notes: Speaker Note: Detail risk mitigations.

## Slide 6
Strategic Recommendations
Actionable Implementation Roadmap
• Step 1: Recommendation: Derate unit operating pressure to 12.0 bar immediately and schedule clamp enclosure installation.
• Step 2: Recommendation: Derate unit operating pressure to 12.0 bar immediately and schedule clamp enclosure installation.
• Step 3: Issue engineering approval note.
• Step 4: Install clamp enclosure within 14 days.
Notes: Speaker Note: Action plan.